## Slide 1
Tobias Mølgaard Nielsen
ADD 2026
14.01.2026
Whole-nanoparticle-ensemble refinements of compositionally complex systems from X-ray pair distribution function data via the Reverse Monte Carlo method

## Slide 2: Compositionally complex systems
Solid solution of 5 or more elements
High-entropy alloy (HEA)
Emerging catalyst materials

## Slide 3
Solid solution of 5 or more elements
High-entropy alloy (HEA)
Emerging catalyst materials
These materials are complex
Detailed structural characterisation remains a challenge
Subtle structural features affect properties
  Chemical short-range order
  Spatial compositional heterogeneities
Deviations from homogeneity affect comparability with theoretical predictions
Compositionally complex systems

## Slide 4
Solid solution of 5 or more elements
High-entropy alloy (HEA)
Emerging catalyst materials
These materials are complex
Detailed structural characterisation remains a challenge
Subtle structural features affect properties
  Chemical short-range order
  Spatial compositional heterogeneities
Deviations from homogeneity affect comparability with theoretical predictions
PDF is a strong tool
Excellent for nanomaterials
Great for local structural features
Small-box modelling not suitable for spatially varying effects
Large-box methods lacking for multimetallic nanoparticles
Compositionally complex systems

## Slide 5
Large-box Reverse Monte Carlo (RMC) modelling
Supercell of thousands of atoms
Random atomic moves
  Atom translations
  Atom-type swaps
Moves accepted based on improvement of fit quality
vs
Reverse Monte Carlo modelling

## Slide 6
Large-box Reverse Monte Carlo (RMC) modelling
Supercell of thousands of atoms
Random atomic moves
  Atom translations
  Atom-type swaps
Moves accepted based on improvement of fit quality
for nanoparticles
Reverse Monte Carlo modelling

## Slide 7
Large-box Reverse Monte Carlo (RMC) modelling
Supercell of thousands of atoms
Random atomic moves
  Atom translations
  Atom-type swaps
Moves accepted based on improvement of fit quality
for nanoparticles
Chemical short-range order
Spatial compositional heterogeneities
Reverse Monte Carlo modelling
Compositional order based on kinetics experiments

## Slide 8
Large-box Reverse Monte Carlo (RMC) modelling
Supercell of thousands of atoms
Random atomic moves
  Atom translations
  Atom-type swaps
Moves accepted based on improvement of fit quality
for nanoparticles
Chemical short-range order
Spatial compositional heterogeneities
Reverse Monte Carlo modelling
Only atom translations
Best fit

## Slide 9
Large-box Reverse Monte Carlo (RMC) modelling
Supercell of thousands of atoms
Random atomic moves
  Atom translations
  Atom-type swaps
Moves accepted based on improvement of fit quality
for nanoparticles
Chemical short-range order
Spatial compositional heterogeneities
Reverse Monte Carlo modelling
Atom translations Atom swaps
Warren-Cowley
short-range order parameter

## Slide 10
Refining against simulated PDFs PdPt
Testing the method
Simulate PDF
Refine against simulated PDF

## Slide 11
Refining against simulated PDFs
PdPt
Testing the method
Refine against simulated PDF
Refined

## Slide 12
Refining against simulated PDFs PdPtRh
Testing the method
Refine against simulated PDF of core@shell
Refined
PDF simulation core@shell
Treat Rh as Pd
Simulated refinement results
RMC able to reproduce compositional ordering
Contributions of neighbouring elements difficult to separate
  WC analysis of pseudo-binaries helpful

## Slide 13
PdPt
Experimental refinement results
Only atom translations

## Slide 14
PdPt
Experimental refinement results
Only atom translations
Best fit

## Slide 15
PdPt
Experimental refinement results
Atom translations
Atom swaps

## Slide 16
PdPtRh
Experimental refinement results
Atom translations
Atom swaps

## Slide 17
PdPtRh
Experimental refinement results
Atom translations
Atom swaps
First nearest neighbour shell
Second nearest neighbour shell

## Slide 18
PdPtRh
Experimental refinement results
Atom translations
Atom swaps
Starting
Refined
Minimum in refinement space where Pt forms a shell-like architecture
Decreased Pt-content in outer layer observed for all starting configurations

## Slide 19
PdPtRhRu & PdPtRhRuIr
Increasing the complexity
PdPtRhRu
PdPtRhRuIr

## Slide 20
PdPtRhRu
Increasing the complexity

## Slide 21
PdPtRhRuIr
Increasing the complexity

## Slide 22
In summary
The challenges
Subtle structural features affect properties
  Chemical short-range order
  Spatial compositional heterogeneities
Deviations from homogeneity affect comparability with theoretical predictions
The presented work
RMC methodology able to identify chemical short-range order and potential core@shell-ish behaviour
    Even for 3 nm sized nanoparticles
    Effects eluding conventional techniques
      Separation of atoms of similar Z difficult with X-rays

## Slide 23
Thank you for listening!

## Slide 24
Element | Neutron coherent scattering length (fm)
Ir | 10.6
Pd | 5.9
Pt | 9.6
Ru | 7.0
Rh | 5.9